**Section 218.786 Surface Preparation Materials**

Every owner or operator of a motor vehicle refinishing operation only shall use surface preparation materials that never exceed the following VOM content limitations for the specified substrate:

|  |  |  |  |
| --- | --- | --- | --- |
|  |  | kg/l | (lb/gal) |
| a) | Plastic parts | 0.78 | (6.5) |
|  |  |  |  |
| b) | Other substrates | 0.17 | (1.4) |

(Source: Added at 19 Ill. Reg. 6848, effective May 9, 1995)